## Slide 1: A22-A25
2h strip
2h anneal 500C
375C 40N 15min
Sub 1N fail

## Slide 2
A22
Post Pull Test
Better alignment of Pads

## Slide 3
A22 Nearside
Post Pull Test
Better alignment of Pads

## Slide 4
A22 Nearside
Post Pull Test
Better alignment of Pads
Not much of a difference vs the non-annealed where vias have broken off.
Vias have height of 5.9um
Vias with misalignment are 7.6um.
Visually inspecting shows that top of the vias
7.6um
5.9um

## Slide 5
A22 Farside
Post Pull Test
Better alignment of Pads
Notes: Total of 28 Glass failures
Failure of gold is more common. ( approx. 120)
Minimal number of titanium-gold failure (3)

## Slide 6
A22 Nearside Pad 1
Post Pull Test
-0.369891 um
-0.556657 um
-0.371221 um
--0.427889um
Notes: What this shows is that majority of failures still occur in the gold layer – not down to the adhesion layer – need to support it more.
Either make the vias larger or do some bevelling (may not be possible with the process)
Bottom of vias is -0.2um deeper than the area removed with the PEVCD – but still not to adhesion layer.
Same failure as without anneal.

## Slide 7
A22 Nearside Pad 7
Post Pull Test
-0.541437um
-0.787184um
Notes: What this shows is that majority of failures still occur in the gold layer – not down to the adhesion layer – need to support it more.
Either make the vias larger or do some bevelling (may not be possible with the process)
Bottom of vias is -0.2um deeper than the area removed with the PEVCD – but still not to adhesion layer.
Same failure as without anneal.

## Slide 8
A22 Nearside Pad 8
Post Pull Test
-0.53957um
-0.503499um
Notes: What this shows is that majority of failures still occur in the gold layer – not down to the adhesion layer – need to support it more.
Either make the vias larger or do some bevelling (may not be possible with the process)
Bottom of vias is -0.2um deeper than the area removed with the PEVCD – but still not to adhesion layer.
Same failure as without anneal.

## Slide 9
A22 Farside Pad 2
Post Pull Test
Better alignment of Pads
-4.88138um
-0.474777um
-4.49165um
-0.351009um
-0.737305um
-0.780919um
Notes: Definite signs of glass failure

## Slide 10
A25 Nearside Pad 2
Post Pull Test
Better alignment of Pads
6.53728um
8.28577um
9.30099um
8.33178um
8.71722um
Notes: Definite signs of glass failure

## Slide 11
A
B
A
B
Delamination of lower layers pulling up the height
Failure seen in Glass (3),
Gold Via (2) (Bulk gold)
A22 Farside Pad 2
Post Pull Test

## Slide 12
A
B
A
B
Pulled Up PECVD
Delamination of lower layers pulling up the height
Failure seen in Glass (1),
Gold Via (2) (Bulk Gold)
Gold-Titanium Layer (1)
A22 Farside Pad 2
Post Pull Test
-1.2um

## Slide 13
A
B
A22 Farside Pad 2
Amount of Gold-Gold Bonding
9 Vias gold failed
9 Vias glass failed
1 Via titanium-gold failed

## Slide 14
A25 Farside Pad 7
Post Pull Test
-0.2984um
-0.354626um
6.548um
-0.5135um
-0.2292um

## Slide 15
PECVD Coating
Layer beneath titanium
Gold
Adhesion Layer
A25 Farside Pad 7
Post Pull Test

## Slide 17: Thoughts so far
Bonds are mainly failing in the gold
As the bond is pulled, the gold stretches and hence shows extension of 0.2um above the bottom.
  Sometimes PECVD remains attached on top, sometimes flakes off
  Curves up the gold layer underneath
2 Main modes of failure, gold failure and glass failure
Glass failure is created right underneath each via, and pulls out some glass from underneath.

## Slide 18
A25
Post Pull Test
Better alignment of pads

## Slide 19
A25 Farside
Post Pull Test
Better alignment of pads

## Slide 20
A25 Nearside
Post Pull Test
Better alignment of pads

## Slide 22
A25 Farside Pad 8
Post Pull Test

## Slide 24: Summary
Annealing has changed the failure point
  No longer seeing failure in titanium, but earlier up
  No 1um ‘nubs’ on top of PECVD
Bond is also weaker than before
Still see some signs of bonds failing in the glass layer.