## Slide 1: 44-53
320C 40 N 15 Min
Pre Anneal: 4N
Anneal: 500C 12H
Post Anneal: 3N

## Slide 2
Alignment and Bonding
44 On bottom, this is the first bond.
Orange Area is where copper pad presses down

## Slide 3
53 Backside
Post Bonding

## Slide 4
44 Backside
Post Bonding

## Slide 5
53 Backside
Pull Test Pre Anneal Progression 1-4N

## Slide 6
44 Backside
Pull Test Progression 1-4N

## Slide 7
53 Backside
Post Anneal

## Slide 8
53 Backside Farside
Post Anneal

## Slide 9
44 Backside
Post Anneal

## Slide 10
44 Backside Nearside
Post Anneal
Notes: Webbing helps to protect the inner material by distributing the pressure more evenly

## Slide 11
53 Backside
Pull Test Post Anneal Progression 1-3N

## Slide 12
53 Farside

## Slide 13
44 Backside
Pull Test Post Anneal Progression 1-3N

## Slide 14
44 Nearside

## Slide 15
53 Farside Pad 2

## Slide 16
A
B
A
B

## Slide 18
53 Farside Pad 6

## Slide 19
A
A
B
B

## Slide 21
44 Nearside Pad 6

## Slide 22
44 Nearside Pad 3

## Slide 23
44
53

## Slide 24: Summary (Pull Test Failure)
Minimal formation of conchoidal fractures during bonding process
  Any large glass fractures (44Farside Pad 1-3) occurs from pull test
  Strongest bonds formed here
Iridescence still seen after bonding
  Is not necessarily a point of failure
Only 1/32 pads has delamination occurred, but was point of failure for that bond.
Pressure is applied quite evenly, but still results in uneven bonding – on both sides, the large glass fractures are along 1 edge
  Flip the strips after bonding each side, and halve the time.

## Slide 25: Summary (Anneal)
Anneal causes compound between titanium and gold to form
  Responsible for change in colour
  But on the metal 1, is responsible for rings to form around the bases of vias
  In most cases, this is a point of failure into glass, may be pre-stressing the glass there and forming fractures