## Slide 1: A21-A10
Bonded at 375C, 40N 15 mins
Failed at 2N

## Slide 2
A21 (Front)
Post Pull Test

## Slide 3
A21

## Slide 4
A10 (Front)
Post Pull Test

## Slide 5: Summary
Good bonding occurs on all pads
Quite Clearly failure is occurring at titanium-gold layer, and removing portions of PECVD with it
On Pad 9, gold-gold interface is the strongest, while failure occurs at the titanium-gold layer.
Uniform bonding seen across all pads – very similar modes of failure.